Synthesis of Poly (N-Substituted imine)  Acryl Amides derivatives from poly acryloyl hydrazine

Entesar  O. AL- Tamimi               &                         Samea'a J. AL- Biaty

University of Baghdad, College of Since     University of Baghdad, College of Since for Women

(NJC)

# (Received on     20 /7  /2005)		(Accepted for publication on   4 / 3 /2006)

Abstract

Reaction of poly (acryloyl chloride ) with hydrazine gave Poly ( acryloyl hydrazine)  which upon treatment with various aldehydes and ketones afforded the corresponded Schiff bases polymers containing pendant amine which added good physical properties and high thermal stability. FT-IR spectrum , C.H.N analysis , softening point ,  melting point and solubility were used to characterize the synthesized polymers .

الخلاصة                                                                                                               تم في هذا البحث مفاعلة بوليمر الاكريلويل كلورايد Poly acryloyl chloride   مع الهيدرازين المائي ليعطي بولي اكريلويل هايدرازين Poly ( acryloyl hydrazine ) ومن ثم مفاعلته مع الالديهايدات والكيتونات المختلفة ليعطي ثماني بوليمرات جديدة بشكل قواعد شيف حيث تحوي سلسلتها البوليمرية على مجموعة امينية  متدلية التي اضافت الى هذه البوليمرات صفات فيزيائية جيدة من استقرارية وثبات حراري عالي ، تم تشخيص المركبات المحضرة باستخدام طيف الـ FT – IR  وتحاليل الـ C , H , N ودرجات التلين ودرجات الانصهار والذوبانية وقد دلت النتائج المستحصلة على صحة التراكيب المقترحة  .

Introduction

Acryloyl chloride can be polymerized easily to linear polymer at room temperature by exposure to ultra – viotet light in quartz  tubes (1). Poly acryloyl chloride can also be prepared by treating poly (acrylic acid) with thionyl chloride (2).

Other route to prepare poly (acryloyl chloride) is by photoinitiated polymerization of acryloyl chloride (3),  from which polyamide (PA) was prepared , which is known by   the trade name nylon , and it consists of highly ordered molecules of  high tensile strength.Amides can also be prepared from acids by treatment with thionyl chloride and then with ammonia (4)

The acrylamide solution is stabilized by oxygen and small amounts (25–30) ppm based of acrylamide of cupric ion. Several other types of stabilizers, such as ferric ion (5,6) and ethylenediamine tetracetic acid (EDTA) (7,8,9),Sulfate salt of acryamide can be used  as a base on an ion – exchange colum (10) and N – substituted acrylamides (11) . So poly amides were synthesized as the same route of amide, many main routes have been mentioned to prepare these compounds (12 – 17).

One of these routes which was used in this paper was from poly acryloyl chloride with hydrazine to give poly (acryloyl hydrazine)

(–   CH2 – CH–  )n  + NH2 – NH2  ( –CH2 –CH–)n

(                                                                                (

C =0                                                      C=0             comp (I)

(                                                           (

Cl                                                           NH – NH2

Modification of polymer I to polymers containing pendant N –substituted amine groups give poly Schiff bases which known to posses  biological activity behavior (18 – 24).

Experimental

Melting points were determined on Gallen kamp Melting points apparatus (MFB – 600), Softening points were determined using Reichert thermovar, Sp1 10/0.25, 160. Elemental analysis of compounds was carried out on C.H.N.S – O, EA7708 Elemental analyzer, CARLO – ERBA instruments, and FT – IR were preformed using FT- IR absorption spectra , KBr discks were used on a RT-IR- 84005 , FOURIER Transform infrared spectrophotometer. SHIMADZU

Preparation of poly (acryloyl hydrazine)(25) ٍِ[I]

A mixture of poly (acryloyl chloride) (0.1mole) and hydrazine hydrate (99%) (0.1mole) in dimethylformamide (DMF) (25 ml) was refluxed  for 12 hrs. After cooling the excess of solvent was removed under vacum and the solid separated was filtered and purified by dissolving at DMF and reprecipitating from acetone. Conversion of yielded polymer was (65%).All physical properties are listed in Table (1, 2) . The FTIR absorptions for the prepared  polymer is shown in Figure (1).

Preparation of N – (substituted imine ) acryl amide[ poly chiff bases]  [ 2 – 9] (26):

Compound [1] (0.01 mole) was dissolved in (20 ml) of dry THF, appropriate aliphatic and aromatic aldehydes and ketones (0.01mole) was added to the mixture, that has been refluxed for  (8 – 12) hrs and cooled. The product was precipitated and filtered off, then  purified from appropriate solvent .All physical properties are listed in Table (1,2) the

FT–IR absorptions spectra for the prepared polymers are shown in Figs (2 – 9).

Results and discussion

Although there are several procedures for the preparation of N – substituted amides (7, 8, 9),, one of them was found suitable for the preparation of poly N – amino acryl amide (or poly acryloyl hydrazine) from reaction of poly acryloyl chloride with hydrazine. The mechanism of the condensation reaction is shown in schem -1- :-

All physical properties and elemental analysis for poly acryloyl hydrazine (I) are listed in Tables (1 – 3) .The FT–IR spectrum show absorption band at 3400 – 3450 cm-1 for NH2 group and at 3317 cm-1 for N – H group , and the absorption band around 2343 cm-1 due to stretching for primary and secondary amines , the FT – IR spectrum showed strong absorption band in the region 1690 cm-1 which is typical for the C=0 stretching vibration of carbonyl amide .The chemical reactivity of the NH2 group in compound (I) plays a significant role in using this compound as a good synthon in the synthesis of new schiff bases as poly N –(substituted imine) acryl amide or poly  N- hydrazines acrylate by reaction of compound (I) with various aldehydes and ketones in dry THF. The FT – IR spectra of polymers (2 – 9) show strong absorption band in the region 1662 – 1687 cm-1 which are typical for the C=N stretching vibration of poly N- substituted imine (poly hydrazones ) 27. In the spectra of the N – acryl hydrazones the absorption band of these groups are shifted to higher frequency and appear at 1700 – 1701 cm-1. .28.It is know that N – acryl hydrozonescan exist in four stereoisomeric forms due to geometrical isomers about the C=N band ( E and Z – isomers) and rotational (conformational) isomerism due to hindered amide rotation around the C – N band of the acryl fragment29 – 30  . In The FT – IR spectra 31 of the poly N- substituted imine which contain N – acryl hydrazones the stretching vibrations of the C=0 group appear as doublet absorption band in the region 1700 – 1660 cm-1 (table 4). Associates with an intermolecular hydrogen band of the type C=0 ……... H – N are absent in solution since the appearance of the spectrum is not changed with dilution. These poly hydrazones acrylate were characterize by useing physical properties and elemental analyses and structures and FT–IR spectray all these characterized listed in tables(1–4) and in Figs (2–8) .         Scheme (2) summarized all the performed reactions in this work

Scheme-2-

All aliphatic aldehydes and ketones have  a good conversion in comparison with  aromatic aldehydes and ketons as can be seen in the following  arrangement

This arrangement is due to steric hindrance and electronic effect. The solubility and melting points of all prepared poly N – (substituted imine ) acryl amides indicate the formation of  high thermal stable polymers .

Table 1: Physical properties of prepared poly acryl hydrazine and its derivatives

| Comp No. | Poly | = R Substituted | Conversion % | Co lour | Softening point S.P. C( | Melting point Tm C( |
| --- | --- | --- | --- | --- | --- | --- |
|  | acryl hydrazine |  | 65 | Yellowish |  | Dec. |
|  | N- (methyl imine) acryl amide |  | 89 | Red | 260-280 | >360 |
|  | N-(ethyl imine) acryl amide |  | 63 | Yellow | 154-170 | >360 |
|  | N-(pheny imine ) acryl amide |  | 48 | Yellow | 260-285 | >360 |
|  | N-(o-nitro pheny imine) acryl amide |  | 29 | Yellow | 200-215 | >360 |
|  | N,N-(methyl ethyl imine ) acryl amide |  | 53 | Yellow - reddish | 180-205 | >360 |
|  | N,N-(Diethyl imine )acryl amide |  | 50 | Yellow - reddish | 240-256 | >360 |
|  | N,N-(methyl phenyl imine) acryl amide |  | 30 | Yellow | 200-215 | >360 |
|  | N,N-(ethyl –o-hydroxy phenyl imine) acryl amide |  | 44 | Yellow | 260-280 | >360 |

Table 2: Solubility of prepared poly – N – (substituted imine ) acryl amide.

| Comp No. | MeOH | EtOH | THF | DMF | CHCl3 | CCl4 | (CH3)2CO | (C2H5)2O | C4H4O2 | PhCH3 | C6H6 | C6H12 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | – | – | + | ++ | – | – | – | – | – | – | – | – |
|  | – | – | + | + | – | – | – | – | – | – | – | – |
|  | – | + | + | + | – | – | + | + | – | – | – | – |
|  | – | + | + | + | – | – | + | + | – | – | – | – |
|  | – | + | + | + | + | – | + | – | – | + | + | – |
|  | + | + | + | + | – | – | + | – | – | – | + | – |
|  | – | – | – | + | – | + | + | – | – | – | – | – |
|  | + | + | + | + | – | – | + | – | + | + | – | – |
|  | + | + | + | – | + | + | + | + | – | + | – | – |

C6H12:Cyclohexane

C4H8O2:Dioxane

Table 3: Elemental analyses of poly acryl hydrazine and some of poly – N – substituted imine acryl amides.

| Comp No. | Elemental analyses | C % | H % | N% |
| --- | --- | --- | --- | --- |
|  | Calc. Fou. | 41.86 42.09 | 6.98 5.87 | 32.56 31.98 |
|  | Calc. Fou. | 53.57 53.09 | 7.14 7.55 | 25.01 25.00 |
| 4. | Calc. Fou. | 68.97 68.16 | 5.75 5.24 | 16.09 15.87 |
| 6. | Calc. Fou. | 60.00 59.76 | 8.57 8.43 | 20.00 20.41 |
| 8. | Calc. Fou. | 70.21 70.01 | 6.38 5.98 | 14.89 14.28 |

Calc. = Calculated

Fou. = Found

Table 4: FT-IR spectra of poly acryl hydrazine and its derivative

| Comp. No. | =R | (N-H) cm-1 | (C-H) ar.cm-1 | (C-H) Vinyl.cm-1 | (C-H) allph. cm-1 | (C=O) cm-1 | b(N – H) cm-1 | (C=C) ar.cm-1 | (C-N-N) (O-C-N) cm-1 | (C=N) cm-1 | Others cm-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 3317 |  |  | 2750 2890 | 1690 | 2343 |  | 1430 1350 | 1668 | V – NH2 3400 - 3450 |
|  |  | 3413 |  | 3022 | 2927 2850 | 1701 | 2345 |  | 1420 1373 | 1670 |  |
|  |  | 3340 |  | 3100 | 2920 2835 2736 | 1676 | 2364 |  | 1394 1326 | 1622 |  |
|  |  | 3411 | 3236 | 3056 | 2927 | 1637 | 2376 | 1612 1508 1490 | 1448 1363 | 1627 |  |
|  |  | 3473 | 3178 | 3020 | 2937 | 1701 | 2345 | 1610 1590 1508 | 1357 1332 | 1629 |  |
|  |  | 3433 |  |  | 2933 2897 | 1701 | 2345 |  | 1442 1346 | 1637 |  |
|  |  | 3315 |  |  | 2990 2877 2812 | 1700 | 2345 |  | 1382 1355 | 1629 |  |
|  |  | 3310 |  |  | 2970 2810 | 1701 | 2345 |  | 1410 1323 | 1687 |  |
|  |  | 3303 | 3238 |  | 2999 2935 2877 | 1710 | 2345 | 1610 1508 1490 | 1448 1373 | 1629 | V- OH Phenolic 3530 |

Figure (5) FT-IR spectro of N-(o-nitro pheny imine) acryl amide polymer

Figure (6) FT-IR spectro of N,N-(methyl ethyl imine ) acryl amide polymer

Figure (7) FT-IR spectro of N,N-(Diethyl imine )acryl amide polymer

Figure (8) FT-IR spectro of N,N-(ethyl –O-hydroxy phenyl imine) acryl amide polymer

References

- R .C. Schutz , R .C.Etzer,W. Kern ,Makrol.Chem., 1961 ,42,189 .

- L .A . R . Hall , W . J .Belanger , W.Kirk,Y & A . Sundstrum , J. Appl. Polym. Sci, 1959, 2, 254  .

- G .G. Egorova , I .I .Mignnova , I.V.Mukhina, & A .Y.Bilibin , Russian J. Appl. Chem., 2002, .Jan .75, 1, 124.

- D .C.Macwilliams , R .H. Yocum and E . B . Nyquist .eds ,Fundemental Monomers”  (1973) ,Vol.1, Makcel Dekker pp.1 – 197, New York .

- P.J. Achorn American Cyanamide ,Co.Stamford.Conn. Unpublished results(1977).

- E.Collinson & F .S. Dainton ,Nature, 1956 , 177,1224 .

- U.S.Pat.,2917, 477T. J.Suen & R.L.Webb to American Cyanamide ,Co .(1959).

- J.B.Friend & A .E.Alexander , J . polym.Sci., 1968 , part   a;16, 1833.

- H. Warson, reactive Derivatives of Acryl amide & allied products, Solihull Chemical Seryice Solihull,UK.(1975) .

- D C.Macwilliams, & M. Grayson, ed,Kirk – Othmen , Encyclopedia of Chemical Technology 3rd ed,Vol.1,John Wily & Sons . Inc.New York. (1978) ,p298 – 311.

- S.Gabriel and TA, Muas, Ber, 1966, 32, 849.

- D .H.Harms , Anal,Chem., 1953, 25, 140 .

- W.M.Kulicke, R .Kniewske , & J. Klenn prog. poly Sci, 1982 , 8 , 373.

- F.Sanda &T.Endo J.Synth , Org ,Jpn, 2001, 59, 7.

- M.Bryiak,I.Ganacaz & G.Pozniak, Eur.polym.J., 2002 , 38, 717.

- O.M.Ekiner & G.Vassiliators, J.Member,Sci, 2001, 189(1), 71.

- A .A.Abdel Hafez , Qatar Univ.Sci. J., 1994 , 14c, 108 .

- S.K.Chandhary,M.Chandhry,A.Chandhary & S.S.Parmer, J.Pharm Sci., 1978, 67, 1507

- K.H.Sinnur,S.Siddappa,S.P.Hiremath&M.G.Purohit, Indian J.Chem, 1986, 25B, 716 .

- M.Y.Yousif, A.M.Ismail,A.A.El-Eman & M.M. El–Kerdawy, J.Chem.Soc, 1986,  Pok .8(2), 183, .

- B.N.Goswami, J.C.S.Kataky & J.N. Baruah , J. Hetrocyclic Chem., 1984 , 21, 1225

- R.N.Goswami ,J.C.S.Kataky , J.N. Baruah & S.C.Nath., J. Hetrocyclic  Chem. 1984 ,21,205 .

- I.F.Mustafa ,A .T.Atto & H.Y.Ahmed, Iraqi J.of Chem., 2001, 27 (3) , 695.

- C. Parkany & D.S.Schmidt , J. Hetrocyclic Chem.,  2000, 37, 725 .

- S.Bahadur , A.K.Goel & R.S.Narva, J.Chem., 1976 , 1,111, 950 .

- R.M.Silverstein ,G.C.Bassler, &T.C.Marrill,Spectrometric Identification of organic compounds” (Russian translation (, Mir,Moscow (1977).

- S.I.Yakimovich ,V.N.Nikolaev , &O.A.Afonina , Zh. Org. Khim, 1979, 15, 922.

- Yu.P.Kitaev & B.I.Buzykin, Hydrazones (in Russian (, Nauka , Moscow (1974)

- K.N.Zelenin ,V.V.Pinson ,A.A.Potekhin ,I.P.Bezhan ,V. A. Khrustalev, & P.S.Lobanov , Zh .Org. Khim.,  1978 , 14, 490.

- S.A.Rutavichyus , S.P.Valyulene & V.V.Mozolis , Zh.Org. Chem., 1987, 23, 1198 .

- V.I.Kelerev, M.A.Silin, I. G. Kotova, K.I.Kobrakov,I.I.Rybina &V.K.Korolev , Chem . of Hetrocyclic Compounds, 2003 , 39(2).